## Slide 1: OPTICAL PROPERTIES OF SOLIDS
OPTICAL SPECTROSCOPY THEORY
(1950-1960)
Mainly R and T  Band structure calculations
 One-electron approximation
 Semi-empirical models
Microscopic interpretation of the fundamental characteristics of the optical response in solids
after 1960
 Modulation spectroscopy  Self-consistent methods
(TR, ER, WLM, PR, PZR, ,,,)  Ab-initio calc. (total energy ,
 Spectroscopic ellipsometry (SE) density functional….)
 Photoluminescence spectr. (PL)  Surface and interface prop.
 Raman spectr. (RS)  Many-bodies, correlations
 Photoemission spectr. (PES)  Molecular dynamics
 Electron spectroscopies (EELS, Auger)
 New growth and processing techniques
(epitaxy Q-size structures)
 New light sources (synchrotron, laser CW and pulsed,…)
 Microprobes (HRTEM, STM, AFM, SNOM, …)

## Slide 2: Interaction of electro-magnetic field with matter
In linear materials, the polarization density (in coulombs per square meter) and magnetization density (in amperes per meter) are given by:
and the and fields are related to and by:
where:
χe is the electrical susceptibility of the material,
χm is the magnetic susceptibility of the material,
is the electrical permittivity of the material, and
μ is the magnetic permeability of the material

## Slide 3: Maxwell Equations
In non-dispersive, isotropic media, ε and μ are time-independent scalars, and Maxwell's equations reduce to
In a uniform (homogeneous) medium, ε and μ are constants independent of position, and can thus be furthermore interchanged with the spatial derivatives.
More generally, ε and μ can be rank-2 tensors (3×3 matrices) describing birefringent (anisotropic) materials.

## Slide 4: REAL AND COMPLEX FORMALISM
In the case of time-dependent e.m. fields, there will generally be a phase shift between the motion of the charge carriers and the electric field E (similarly to what happens in A.C. circuits). In such cases the complex formalism is particularly convenient to describe phase shifts, and in addition to describe dispersion and absorption effects at the same time. Complex fields are usually defined, the real parts of which have physical meaning and are the ones involved in Maxwell’s eqs.
REAL FORMALISM
E = EO cos t x = C EO cos (t + ) x’ = - C  EO sen (t + )
J = eNx’ = - eNC EO (sen t cos  + cos t sen )
90° out of phase vs E in phase with E
(polarization current - no dissipation) (conduction current – dissipation)
COMPLEX FORMALISM

## Slide 5
1()   () describes the dispersion processes, i.e. the displacement r of the charges in-phase with E p = e r =  E
2()  4  ()/ describes the energy absorption, i.e. the velocity v of the charges in-phase with E
W = < J  E > =  < E2 > + 1 < E/t E > =  < E2 > + 0
Only for  = 0 (static field)   0 is due to free-carriers (conductor) and 1   to bound- carriers (dielectric). For  > 0 the distinction between free- and bound-carriers is meaningless (for   the charges are all “free”).
In order to elucidate the meaning of 1 and 2 let us consider the Maxwell eqs.:
with  1 + i 2 =  - i   complex optical conductivity
with  1 + i 2 =  + i 4  / complex dielectric function

## Slide 6
 E, (), () appearing in the Maxwell eqs. are macroscopic quantities, average on volume elements V (with   V  a3) of microscopic quantities which vary rapidly on the atomic scale.
 The displacement of one point-charge does not depend on E but on Eloc, which can differ greatly from E and which should be generally calculated in a self-consistent way.
 In an anisotropic medium
 ()  () complex dielectric tensor
1() and 2() are always symmetric tensors they can be diagonalized with respect to principal axes, depending on . Generally the directions of the principal axes are different for 1() and 2() , but they do coincide for crystals with symmetry at least as high as orthorhombic. In a cubic crystal ij reduces to a scalar quantity.





 In a nonlinear dielectric medium, it is possible to expand the relation between P and E in a Taylor series about E = 0. Thus
P = ( E + 2) E2 + 3) E3 +…)
where the (n) coefficient describes the n-th order nonlinear effect. The D’Alembert equation is not applicable to e.m. waves in nonlinear media. However, Maxwell’s equations can be used to derive a nonlinear partial differential equation that these waves obey.

## Slide 7: KRAMERS-KRONIG RELATIONS
1() and 2() are not independent quantities, being related one to the other by the integral relations, the so called Kramers-Kronig relations. These relations follow rigorously from the requirement of causality (i.e., there can be no effect before the cause) and apply to the real and imaginary part of whatever linear response function. Thus, the complex dielectric function obeys the following relations
where P stands for the principal part of the integral.
Also the Fresnel coefficient expresses the linear relation between incident and reflected electric field amplitudes which obey causality a dispersion relation exists which connects its real and imaginary parts. Using the normal incidence reflectivity , the dispersion relation between the absolute value R and the phase angle  should be written as:

## Slide 8: DIELECTRIC RESPONSE OF SOLIDS
amplitude, polarization and initial phase
complex wavevector q = q1 + i q2
From the Maxwell’s eqs. the wave equation (d’Alembert eq.)
e.m. wave propagating in a absorbing medium
attenuation of wave amplitude + dephasing between field and medium response
(i.e.: A.C. circuits)
usefulness of complex formalism.
A solution of the d’Alembert eq. Is a monochromatic plane wave (transverse, because  E = 0):
Homogeneous, isotropic, non-magnetic, charge-free medium
Complex dielectric function
with q= 2u/
linear response
= 1,q) + i 2,q)
dispersion absorption

## Slide 9
By inserting the plane-wave complex solution in the Maxwell eqs., we obtain:
 (,q) 2 = c2 q q dispersion relation




The  and q dependence of  (,q) (or  (,q)) describe the time and the spatial dispersion of the material, respectively. If  >> a (where a is a natural length in the medium, i.e. atomic dimension or lattice parameter) the space variation of  can be neglected  (,q) =  () (this is not possible at X-ray wavelengths).
Moreover, for q  0 (  ) the transverse and longitudinal response coincide, i.e. the medium cannot distinguish between electric fields parallel or perpendicular to q
direct comparison between EELS spectroscopy and optical spectroscopy
We note that the wave dispersion relation does not imply in general a connection between time-dispersion and spatial-dispersion. In principle, it is possible to investigate separately the temporal response of a medium (and hence the time-dispersion in ) by subjecting it to a spatially uniform field that oscillates in time, or the spatial response (and hence the spatial dispersion in q) with a static field that is spatially periodic.

## Slide 10
Una funzione d’onda è caratterizzata da due grandezze coniugate:
frequenza e lunghezza d’onda.
La relazione tra queste due grandezze dipende dalla natura della radiazione
Frequenza e lunghezza d’onda sono altresì legate ad un’altra coppia di grandezze coniugate, energia e momento, che possono essere usate in sostituzione delle prime senza perdita di informazione.

## Slide 11: SPETTROSCOPIA (e spettroscopie)
Con il termine spettroscopia si intende una grande varietà di tecniche. Se pure il primo riferimento (anche dal punto di vista storico) va alla spettroscopia ottica e agli spettri di emissione o di assorbimento dei gas nel visibile e nel vicino ultravioletto, che per primi hanno evidenziato una struttura discreta dei livelli atomici, si parla oggigiorno di spettroscopia NMR così come di spettroscopia di neutroni.
Si intende come spettroscopia ogni tecnica che fornisce una grandezza risolta spettralmente, ovvero separando le sue componenti a diversa frequenza.
L’esempio più comune è dato dalla radiazione elettromagnetica e dalla sua decomposizione nei diversi colori del visibile, ma il discorso può essere esteso senza salti concettuali a tutte le frequenze e a tutte le grandezze per le quali è possibile definire una frequenza e/o una lunghezza d’onda.
Ogni grandezza in grado di propagarsi nello spazio (radiazione) e che possieda un carattere ondulatorio può essere impiegata per uno studio spettroscopico; nella fattispecie le stesse particelle (quali gli elettroni, i neutroni o i muoni) che possono essere associate ad una funzione d’onda (di De Broglie).

## Slide 12
Numeri d’onda
Energia 104 103 102 101 1 10-1 10-2 10-3 10-4 10-5 10-6
 eV

## Slide 13
donors
acceptors
Fig. 2 Hypothetical absorption spectrum for a typical doped semiconductor and related electronic optical transitions.

## Slide 14: OPTICAL SPECTRA
(R, T, SE, modulation spectroscopy, polarimetry)
complex dielectric function
direct map of the elementary excitations in solids,
weighted with JDOS and transition probabilities
 optical gaps
 interband critical points
 effective masses m*
 vibrational structure
 effects of external perturbations on electronic states
(temperature, E, H, doping, structural and compositional disorder, size,...)
OPTICAL CHARACTERIZATION

## Slide 15: OPTICAL CHARACTERIZATION
 n(), k(), () optical functions
 N, m*,  of free-carriers
 Spatial homogeneity (range 1-1000 nm) and thickness of films and multilayers
 Surfaces and interfaces
(roughness, planarity, anisotropy, traps, transition regions, oxides, overlayers,…)
 Compositional (impuritirs or dopants) and structural defects
 Structural disorder (single-crystal, polycrystal, amorphous,…)
 Phase transitions (structural, magnetic, conductor-insulator, superconductors)
 Dynamical processes associated to the growth (in situ measurements)
 Radiation effects and damages (light, ion and electron beams)

## Slide 16: ADVANTAGES OF OPTICAL SPECTROSCOPY
 It can be used in situ, during growth, fabrication or testing
 It does not require special environments, such as ultrahigh vacuum (UHV),
and may even be useful in hostile environments
 It is nonintrusive and noncontact ( repeatability)
 It may achieve submicron lateral resolution (SNOM  20 nm)
 It can be used to acquire data in real time (i.e., as growth or processing takes place)
 It offers the possibility of depth probe (depending on )
 It presents a wide array of techniques, capable of measuring different properties and parameters (e.g.:optical functions, electronic properties, crystal order, thickness, impurities,composition, surface and interface quality, etc.)
 It has high spectral resolution /  (10-3 vis-UV,  10-5 FFT- FIR)
and high sensitivity to spectral details (derivative techniques)
 It has high sensitivity to the long-range order (disorder), to the thickness ( 1 monolayer),
to impurities ( 1/109)

## Slide 17: LIMITS OF OPTICAL SPECTROSCOPY
 It does not give information on the absolute positions
of the electron energy-levels
 It probes typically more than 10 nm in depth
average response in depth
no detailed information on electronic bonds,
surface structure, short-range effects
 It needs a “model” of the examined sample
(particularly relevant in films and multilayer structures)

## Slide 18: Infrared Spectroscopy
Infrared spectroscopy studies vibrational frequencies of molecules.
The vibrations of molecules are what can help a researcher to determine a specific molecule. The most direct way to obtain the vibrational frequencies is with infrared radiation. A molecule that is said to be “IR active” has a change in its dipole moment as a result of the absorbance of infrared radiation.
A non-linear polyatomic molecule would use the 3N-6 formula to determine the number of vibrational modes.
Water, H2O, would therefore have 3 vibrational modes.

## Slide 19
Water, H2O, would therefore have 3 vibrational modes.

## Slide 20
This is a symmetrical stretch. As you can see, the magnitudes of the arrows indicate that the stretch causes an increase in the dipole moment, pulling the oxygen away from the two hydrogen atoms. Although there is no change in the direction of the dipole moment, there is a change in its magnitude.
This vibrational mode is IR active and would be observed on a spectrum around 3650 cm-1.
+
-
+
-
P
+
+
-

## Slide 21
Water, H2O, would therefore have 3 vibrational modes.

## Slide 22
This is an asymmetrical stretch. This is more difficult to see, however, there is a change both in the magnitude and the direction of the dipole moment.
This vibrational mode is IR active and would be observed on a spectrum around 1690 cm-1.
-
+
-
+
+
+
+
-
+
+
-
P
=

## Slide 23
Water, H2O, would therefore have 3 vibrational modes.

## Slide 24
This is the one bending mode of water. In this mode the direction is unchanged, however as with the symmetrical stretch, the magnitude is changed.
This vibrational mode is IR active and would be observed on a spectrum around 3750 cm-1.
+
-
+
-
P
+
+
-

## Slide 25
absorption intensity ratio (H216O)
v1;v2;v3 = 0.07;1.47;1.00
Main vibrations of water isotopologues
Gas
v1, cm-1
v2, cm-1
v3, cm-1
H216O
3657.05
1594.75
3755.93
H217O
3653.15
1591.32
3748.32
H218O
3649.69
1588.26
3741.57
HD16O
2723.68
1403.48
3707.47
D216O
2669.40
1178.38
2787.92
T216O
2233.9
995.37
2366.61

## Slide 26
Moreover, 3 libration modes also exist.

## Slide 27
In liquid water and ice the infrared and Raman spectra are far more complex than the vapor due to vibrational overtones and combinations with librations (restricted rotations; i.e. rocking motions). These librations are due to the restrictions imposed by hydrogen bonding (minor L1 band 395.5 cm-1; major L2 band 686.3 cm-1
Variations in the environment around each liquid water molecule gives rise to considerable line broadening with vibration shifts in a hydrogen-bond-donating water molecule being greater than in a hydrogen-bond accepting molecule but both acting in the same direction, and accumulating with the number of hydrogen bonds.
The main stretching band in liquid water is shifted to a lower frequency (v3, 3490 cm-1 and v1, 3280 cm-1) and the bending frequency increased (v2, 1644 cm-1) by hydrogen bonding.

## Slide 28
Assignment of the IR vibrational absorption spectrum of liquid water
Wavelength
cm-1
Assignment
Wavelength
cm-1
Assignment
0.2 mm
50
intermolecular bend
1470 nm
6800
av1 + bv3; a+b=2
55 μm
183.4
intermolecular stretch
1200 nm
8330
av1 + v2 + bv3; a+b=2
25 μm
395.5
L1, librations
970 nm
10310
av1 + bv3; a+b=3
15 μm
686.3
L2, librations
836 nm
11960
av1 + v2 + bv3; a+b=3
6.08 μm
1645
v2, bend
739 nm
13530
av1 + bv3; a+b=4
4.65 μm
2150
v2 + L2 a
660 nm
15150
av1 + v2 + bv3; a+b=4
3.05 μm
3277
v1, symmetric stretch
606 nm
16500
av1 + bv3; a+b=5 [526]
2.87 μm
3490
v3, asymmetric stretch
514 nm
19460
av1 + bv3; a+b=6 [526]
1900 nm
5260
av1 + v2 + bv3; a+b=1
Note that a and b are integers, ≥ 0 ms.

## Slide 34
If the wave is homogeneous, i.e. , it holds , where is the unit vector parallel to and then
Thus the wave plane solution should be written as
n determines the phase velocity c/n of the wave in the medium
k measures the attenuation of the wave amplitude with the propagation distance inside the medium
The classical skin depth  , defined as the distance at which the field amplitude drops of 1/e, is  = c/( k)
From
where is the complex refractive index such that
n is the usual refractive index ; k is the extinction coefficient. Thus

## Slide 35: ABSORPTION COEFFICIENT
I0 = incident wave intensity.
 is usually measured in cm-1 (n and k, instead, are dimensionless) . -1 is the penetration depth.
d = optical density (it reflects both the physical chemical properties and the geometry of the medium)
The exponential attenuation of I after a propagating distance d accounts for the phenomenological Lambert-Beer law :
An additional important macroscopic quantity of the medium is the absorption coefficient  , which describes the relative decrease in the wave intensity I with unit distance (in the propagation direction, i.e. // dr). Since the wave intensity (i.e. the power which is incident on the unit area perpendicular to ) is
from the plane-wave solution it follows

## Slide 36
from Maxwell equations:
refractive index
{
OPTICAL MEASUREMENTS OF SILICIDES
The optical response of a material is related to its dielectric function
extinction coefficient

## Slide 37: REFLECTION AND TRANSMISSION
At the interface between two media, the reflected (Ir) and transmitted (It) wave intensities relative to the incident one (I0) are called reflectivity R and transmittivity T. At normal incidence they are given by
Let us consider a sample of material with and thickness d, immersed in air ( = 1) as shown in Figure 1. Coming from air, the near-normally incident beam is split into reflected and transmitted fractions (as determined by R and T) at each interface, giving rise to secondary beams: by summing up all the multiple-reflected and multiple-transmitted elements, which account also for light absorption along the thickness d, we obtain the total intensity reflected from the front surface:
R + T = 1
(energy conservation)

## Slide 52
Interference and Fourier Transform Spectroscopy
  Coherence and Interference
  Interferometry and Interferograms
  Fourier components
      time-dependence of a signal
      resolution
  Fourier Transform Spectroscopy
      Advantages
      Spectrometers
  Conclusions
Notes: Title and presentation

## Slide 53
Phase and Amplitude
Any oscillating quantity A(t) = Aocos (t-k.r+) (for electro-magnetic waves the electric field vector and the magnetic field vector) is characterized by :
  the oscillation frequency 
  the wavelength, /|k| v/
Once the frequency has been fixed (monochromatic wave) and the velocity of propagation “v” is given
  the amplitude = the maximum value Ao
  the phase of the wave 
Of course, the phase definition related to a reference e.g. a second component of the same beam

## Slide 54
The two wave components (A1,A2) recombine at the exit of the interferometer and sum their instantaneous amplitudes: the eventual phase delay of one wave with respect to the other must be taken into account.
Let us consider a wave travelling from a source S to a beam splitter B
S
B
A1
A2
MIRROR 1
MIRROR 2

## Slide 55: Phase modulation : Interferogram

=
=
A
The final amplitude of the out-coming wave is then modulated by the relative phase shift of the two wave components.
When the phase shift (or the delay) of one of the compo-nents is changed (e.g.: by changing the optical path, moving a mirror or intro-ducing a different medium) the amplitude, and then the intensity of the outcoming wave is correspondingly changed.

## Slide 56: Interferogram

## Slide 57: Interferogram
Each component with frequency  and wavevector k = /c is then modulated by the spatial delay z;
The whole beam can be described by the sum (the integral) of all the components;
By considering the intensity of each component (and of the whole beam) one is obtaining a sum of a constant term and a modulated one.

## Slide 58: Interferogram
When the delay z is described as a continuous, linear function of time, one can show that the resulting intensity is also time dependent and corresponds to the Fourier transform of its spectral function.

## Slide 59: Interferogram
The function of time (interferogram) obtained is different depending on the spectral content of the light beam:
A single frequency beam will be modulated as a continuous cosine function;
A spectrum extended over a frequency region will approximate a delta function (pinned at z=0) as better as the frequency region is larger.

## Slide 60: Interferogram and resolution


I()
I(t)
t


I()
I(t)
t

t=2/

## Slide 61: How is Working a Fourier Transform Spectrometer

## Slide 62: Main features of a Fourier Transform Spectrometer
Besides the necessary lamp and detector, the key features of a FTIR instrument are:
  An interpherometer moving mirror whose position can be controlled to a high accuracy (usually such a control is obtained with the help of a laser);
  A sampling and acquisition system which allows to obtain the correct time dependence of the interferogram;
  An analysis system which can perform the FFT (fast Fourier Transformations) and correctly evaluate the corrections (intensity, phase and noise effects introduced by the experimental setup).

## Slide 63: Main features of a Fourier Transform Spectrometer
The interference signal of a laser beam colinear to the light path in the interferometer is used to control the position of the moving mirror with a precision of less than 1 nm;
The same interference fringes of the laser are used for the sampling of the data: according to the Nyquist theorem, one must sample the data at a frequency (at least) double of the maximum frequency of phase modulation;
An usual PC is nowadays enough to perform the mathemati-cal data treatment (and also to control the whole experiment)

## Slide 64: Advantages of FTIR Spectroscopy
The so-called Jaquinot advantage: there is no need of slits which limit the throughput of radiation, so one can have a large signal without affecting the resolution;
The Fellget (multiplex) advantage: the whole spectrum is obtained simultaneously for all the frequencies from a single interpherogram;
Because of the two features above, it is possible to obtain instruments with a much higher resolving power than in dispersive instruments, even when the beam energy is low;
Since mirror mouvements can be very fast (and/or very precise), time resolution is easily implemented.

## Slide 67: Interferogram and resolution
Problem: it is obviously impossible to measure an interferogram developing in time from - to .
What is then the effect of taking a limited portion of signal (let us say from t=- to t=)?
Answer: there is a kind of inverse symmetry between the two conjugated spaces. As shown in the pictures above, inasmuch a structure is narrow on one side, as much its transformed counterpart is extended.
This also means that we can only distinguish among different spectral components close one to the other if the correspon-ding interferogram is wide enough.
Resolution depends on the length of the interferogram

## Slide 68: Interferogram and resolution
As an example let us consider the interferogram obtained by the sum of two components at frequency 1 and 2, respectively. It will consist of the product of two cosine function: one of frequency [v(1+2)/2c] and the other one of frequency [v(1-2)/2c].
The first one is a rapidly varying function corresponding to the interferogram of a single component spectrum with an average frequency between 1 and 2.
In order to discriminate between 1 and 2 one has to wait a time corresponding to the period of the second, slowly varying function, which bring the information about the difference 1- 2.
+
=
| …. t = 4c/v(1-2) … |

## Slide 69: Resolution and Apodization
The truncation of the interferogram at the limits – and + can be viewed as the multiplication of the interferogram by a boxcar function having the same limits.
According to the convolution theorem and considering that the Fourier transform of a boxcar function is the sinc function, the resulting Fourier transform of the considered interferogram is the convolution of the Fourier transform of the whole spectrum with the sinc function with argument (t/).
Since the sinc function introduces some lobes in the spectra of narrow lines, it is sometimes preferred to multiply the interferogram by a function which reduces the intensity to zero at the limits – and +. This can be a triangular function, or an exponential decay, or a combination of function. The effect is the reduction of the lobes, payed by a loss of resolution.
Such an operation is called Apodization.

## Slide 70: Phase correction
All the components of an interferometer introduce, in general, both an intensity correction and a phase contribution to the interference beam. The amplitude (intensity) effects are similar to the ones introduced by any optical device in a spectroscopic experiment, and call for the need of a reference measurement.
The phase effects are peculiar of the use of an interferometer. In general, the phase shift introduced by the optics (mirrors, beam splitter, retardation plates) is a function of the wavelenght and of the experimental geometry (since one has to do with several different optical paths when the light beam is not perfectly collimated) and is adding to the modulation shift intentionally created in the experiment.
The effect of such a situation is that each component is added to form the interferogram with a different phase shift; in other words, both cos- (symmetrical) and sin- (antisymmetrical) functions contribute to the interferogram. It means that both real- and imaginary- components are obtained after inverse FT.

## Slide 71: Phase correction
Since the experiment result is usually an intensity value, just the power spectrum is actually interesting. Nevertheless, the calculation of the phase correction is a necessary step in the process.
Phase spectrum is, in general, a slowly varying function of the frequency; then a low resolution evaluation is enough to have a good correction. Such a spectrum can be interpolated in order to be used for the correction of a high resolution spectrum.
This way of proceeding has two advantages:
  A more efficient averaging of the noise in the spectrum can be achieved using with respect to
  The possibility of dealing with an interferogram not symmetrically displaced around its maximum (which is the ordinary case in the experiments)

## Slide 72: DFFT Discrete Fast Fourier Transform
The need of a discrete sampling of the interferogram data allows the use of a computer and fast algoritmes to make the transformation.
Nevertheless the discrete character of the data introduces some further problems and requires some caution in producing and evaluating the results.

## Slide 73: DFFT Aliasing
The sampling theorem says that the sampling frequency must be the double of the largest frequency max of the signal. That means that, in order to avoid spurious contributions (aliasing), one needs some kind of low pass filter (optical or electrical) which cut the spectrum above max .
Due to the discrete character of the sum, the Fourier transformed function results to be a symmetrical and periodic function in the frequency space, with period 1/2max . (this is way a component with frequency larger than max should be folded and superimposed to the lower frequencies, leading to a wrong spectrum)